LOCATION OF BRONSTED SITES IN DEUTERATED L-ZEOLITE: A COMBINED NEUTRON POWDER DIFFRACTION AND COMPUTER MODELING STUDY

Martucci A1*., Precisvalle N. 1, Fois E. 2, Ardit M. 1, Beltrami G. 1, Pasti L. 3, Suard E. 4 and Tabacchi G*.2

1Department of Physics and Earth Sciences University of Ferrara Via Saragat 1, I-44121, Ferrara, Italy

2Department of Science and High Technology, University of Insubria and INSTM, 22100, Como, Italy

3Department of Environmental and Prevention Sciences, University of Ferrara

4Institut Laue-Langevin, 71 Avenue des Martyrs, 38000 Grenoble, France

*Corresponding authors: mrs@unife.it; gloria.tabacchi@uninsubria.it

Contents:

1. NEUTRON POWDER DIFFRACTION:

Table SI1. Atomic coordinates, fraction and Atomic Displacement Parameters of framework and extraframework atoms of L-LTL.

Table SI2. Atomic coordinates, fraction and Atomic Displacement Parameters of framework and extraframework atoms of ND4-LTL.

Table SI3. Atomic coordinates, fraction and Atomic Displacement Parameters of framework and extraframework atoms of D-LTL.

Table SI4. Framework and extraframework bond distances of L-LTL, ND4-LTL and D-LTL.

2. COMPUTATIONAL MODELS:

Table SI5. Calculated fraction crystallographic coordinates (x, y, z) of D-LTL.

Table SI1. Atomic coordinates, fraction and Atomic Displacement Parameters of framework and extraframework atoms of L-LTL.

| Site | x/a | y/b | z/c | Fraction | Ui/Ue*100 |
| --- | --- | --- | --- | --- | --- |
| KB | 2/3 | 1/3 | 1/2 | 1.0(1) | 1.72(2) |
| KC | 1/2 | 0.0 | 1/2 | 1.0(1) | 3.32(2) |
| KD | 0.2993(1) | 0.0 | 0.0 | 0.85(1) | 8.17(3) |
| Al1 | 0.0933(6) | 0.3570(10) | 1/2 | 0.30(1) | 1.12(3) |
| Si1 | 0.0933(6) | 0.3570(10) | 1/2 | 0.70(1) | 1.12(3) |
| Si2 | 0.1657(6) | 0.4983(2) | 0.2102(13) | 0.78(1) | 1.12(3) |
| Al2 | 0.1657(6) | 0.4983(2) | 0.2102(13) | 0.22(1) | 1.12(3) |
| O1 | 0.0 | 0.2709(13) | 1/2 | 1.0 | 1.18(3) |
| O2 | 0.1639(13) | 0.3278(26) | 1/2 | 1.0 | 1.18(3) |
| O3 | 0.2642(8) | 0.5285(17) | 0.2530(35) | 1.0 | 1.18(3) |
| O4 | 0.1007(10) | 0.4122(8) | 0.3255(19) | 1.0 | 1.18(3) |
| O5 | 0.4247(2) | 0.8493(4) | 0.2730(25) | 1.0 | 1.18(3) |
| O6 | 0.1443(18) | 0.4760(18) | 0.0 | 1.0 | 1.18(3) |
| W1 | 0.0657(11) | 0.0 | 0.0 | 0.22(4) | 12.67(3) |
| W2 | 0.1258(10) | 0.2517(13) | 0.0 | 0.95(3) | 12.67(3) |
| W3 | 0.1295(13) | 0.0 | 0.2486(9) | 0.58(3) | 12.67(3) |
| W4 | 0.1189(10) | 0.0 | 1/2 | 0.64(2) | 12.67(3) |
| W5 | 0.0 | 0.0 | 1/2 | 0.09(4) | 12.67(3) |

Table SI2. Atomic coordinates, fraction and Atomic Displacement Parameters of framework and extraframework atoms of ND4-LTL.

| Site | x/a | y/b | z/c | Fraction | Ui/Ue*100 |
| --- | --- | --- | --- | --- | --- |
| KB | 2/3 | 1/3 | 1/2 | 1.0(1) | 4.20(1) |
| Si1 | 0.0957(6) | 0.3635(8) | 1/2 | 0.70(1) | 1.74(1) |
| Al1 | 0.0957(6) | 0.3635(8) | 1/2 | 0.30(1) | 1.74(1) |
| Si2 | 0.1646(5) | 0.5005(6) | 0.2076(10) | 0.78(1) | 1.74(1) |
| Al2 | 0.1646(5) | 0.5005(6) | 0.2076(10) | 0.22(1) | 1.74(1) |
| O1 | 0.0 | 0.2900(13) | 1/2 | 1.0 | 1.62(2) |
| O2 | 0.1747(4) | 0.3493(8) | 1/2 | 1.0 | 1.62(2) |
| O3 | 0.2625(7) | 0.5251(13) | 0.2292(20) | 1.0 | 1.62(2) |
| O4 | 0.1095(9) | 0.4204(7) | 0.3286(8) | 1.0 | 1.62(2) |
| O5 | 0.4359(4) | 0.8718(7) | 0.2630(4) | 1.0 | 1.62(2) |
| O6 | 0.1412(5) | 0.4780(4) | 0.0 | 1.0 | 1.62(2) |
| N1 | 1/2 | 0.0 | 1/2 | 0.98(1) | 1.25(2) |
| N2 | 0. 294(2) | 0.0 | 0.0 | 0.48(1) | 1.25(2) |
| N3 | 0.125(4) | 0.250(7) | 0.0 | 0.17(1) | 1.25(2) |
| N4 | 0.137(1) | 0.068(3) | 0.318(2) | 0.16(1) | 1.25(2) |

Table SI3. Atomic coordinates, fraction and Atomic Displacement Parameters of framework and extraframework atoms of D-LTL.

| Site | x/a | y/b | z/c | Fraction | Ui/Ue*100 |
| --- | --- | --- | --- | --- | --- |
| KB | 2/3 | 1/3 | 1/2 | 1.0(1) | 5.72(2) |
| Si1 | 0.09394(3) | 0.3575(7) | 1/2 | 0.70(1) | 0.13(1) |
| Al1 | 0.09394(3) | 0.3575(7) | 1/2 | 0.30(1) | 0.13(1) |
| Si2 | 0.1654(4) | 0.4964(7) | 0.2084(8) | 0.78(1) | 0.13(1) |
| Al2 | 0.1654(4) | 0.4964(7) | 0.2084(8) | 0.22(1) | 0.13(1) |
| O1 | 0.0 | 0.2774(8) | 1/2 | 1.0 | 2.10(2) |
| O2 | 0.1654(5) | 0.3307(10) | 1/2 | 1.0 | 2.10(2) |
| O3 | 0.2633(7) | 0.5266(15) | 0.2371(43) | 1.0 | 2.10(2) |
| O4 | 0.1070(7) | 0.4124(8) | 0.3228(12) | 1.0 | 2.10(2) |
| O5 | 0.4359(6) | 0.8718(6) | 0.2630(8) | 1.0 | 2.10(2) |
| O6 | 0.1411(18) | 0.4780(13) | 0.0 | 1.0 | 2.10(2) |
| D1 | 0.0600(6) | 0.5300(7) | 0.2527(5) | 0.58(1) | 8.80(1) |
| D2 | 0.0 | 0.2124(11) | 1/2 | 0.14(1) | 9.43(1) |
| W1 | 1/2 | 0.0 | 1/2 | 0.52(1) | 3.51(2) |
| W2 | 0.2930(3) | 0.0 | 0.0 | 0.40(1) | 2.00(1) |

Table SI4. Framework and extraframework bond distances of L-LTL, ND4-LTL and D-LTL.

| Bond distances (Å) |  | L-LTL | ND4-L |  |  |  | D-LTL |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| T1-O1 |  | 1.662(9) | 1.670(8) |  |  |  | 1.615(10) |  |  |
| T1-O2 |  | 1.641(9) | 1.670(8) |  |  |  | 1.616(10) |  |  |
| T1-O4 [x2] |  | 1.629(9) | 1.681(7) |  |  |  | 1.616(12) |  |  |
| <T1-O> |  | 1.640 | 1.674 |  |  |  | 1.616 |  |  |
| T2-O3 |  | 1.647(9) | 1.710(7) |  |  |  | 1.610(9) |  |  |
| T2-O4 |  | 1.680(8) | 1.670(6) |  |  |  | 1.618(9) |  |  |
| T2-O5 |  | 1.651(9) | 1.740(7) |  |  |  | 1.743(10) |  |  |
| T2-O6 |  | 1.637(13) | 1.700(9) |  |  |  | 1.620(12) |  |  |
| <T2-O> |  | 1.654 | 1.705 |  |  |  | 1.648 |  |  |
| T-O-T angles (°) |  |  |  |  |  |  |  |  |  |
| T1-O1-T1 |  | 128.0(1) | 145.6(9) |  |  |  | 135.6(9) |  |  |
| T1-O2-T1 |  | 146.9(1) | 163.7(1) |  |  |  | 149.3(9) |  |  |
| T2-O3-T2 |  | 138.6(1) | 149.9(1) |  |  |  | 141.7(1) |  |  |
| T1-O4-T2 |  | 143.92(9) | 152.5(7) |  |  |  | 148.7(1) |  |  |
| T2-O5-T2 |  | 142.3(2) | 129.2(7) |  |  |  | 131.1(1) |  |  |
| T2-O6-T2 |  | 151.4(3) | 148.8(2) |  |  |  | 151.2(1) |  |  |
| <T-O-T> |  | 141.8 | 148.2 |  |  |  | 149.9 |  |  |
| KB-O3 [x6] |  | 2.89(1) | 3.18(1) |  |  |  | 2.98(1) |  |  |
| KC-O4 [x8] | 3.29(1) |  |  | N1-O5 [x4] | 2.84(1) |  |  | D2-O1 | 1.19(6) |
| KC-O5 [x4] | 2.95(1) |  |  | N2-O6 [x2] |  | 3.20(1) |  | D1-O5 | 1.09(3) |
| KD-O4 [x4] | 3.15(1) |  |  | N2-N3 [x2] |  | 2.90(1) |  | D1-W1[x4] | 2.09(1) |
| KD-O6 [x2] | 3.01(1) |  |  | N3-N4 [x2] |  | 3.00(1) |  | W1-O5[x4] | 2.71(1) |
| KD-W2 [x2] | 2.86(1) |  |  | N4-N4 |  | 2.74(1) |  | W2-O6[x2] | 3.07(1) |
| W1-W2 [x2] | 3.04(2) |  |  |  |  |  |  | W2-O4[x4] | 3.20(1) |
| W1-W3 [x2] |  |  | 2.22(1) |  |  |  |  |  |  |  |
| W1-W3 [x4] |  |  | 2.79(1) |  |  |  |  |  |  |  |
| W2-W3 [x4] |  |  | 2.96(1) |  |  |  |  |  |  |  |
| W5-W3 [x12] |  |  | 3.05(1) |  |  |  |  |  |  |  |
| W5-W4 [x6] |  |  | 2.20(2) |  |  |  |  |  |  |  |
| W3-O1 |  |  | 3.23(1) |  |  |  |  |  |  |  |
| W4-O1 |  |  | 2.80(1) |  |  |  |  |  |  |  |

2. COMPUTATIONAL METHODS AND MODELS

First principles studies of D-LTL were performed adopting the experimentally determined cell parameters. The stoichiometry of the unit cell was K2[Al9Si27O108]D16D2 , while the simulation cell was doubled along the c direction. No symmetry constraints was imposed on the atomic positions, and only the cell was kept fixed. Electronic interaction was treated within the Density Functional Theory (DFT) adopting the PBE-D2 approximation. Norm Conserving pseudopotentials were used for K, Si and Al atoms, while ultra-soft pseudopotentials were used for O and H atoms.  Electronic states were expanded in plane waves using a kinetic energy cut off of 30 Ry (240 Ry for the electronic density). Periodic boundary conditions were adopted in all calculations.

Table SI5. Calculated fraction crystallographic coordinates (x, y, z) of D-LTL.

Atom Site  x/a      y/b      z/c

Si   T1     0.3467   0.2646   0.4797

Si   T1     0.0879   0.7372   0.5299

Si   T1     0.2561   0.9082   0.5210

Si   T1     0.7195   0.0952   0.4637

Si   T1     0.8934   0.2596   0.4616

Si   T1     0.9058   0.6535   0.4744

Si   T1     0.6340   0.7454   0.5237

Si   T1     0.6349   0.9109   0.5225

Si   T1     0.2504   0.3479   0.5453

Al   T1     0.0797   0.3474   0.5503

Al   T1     0.3456   0.0990   0.5196

Al   T1     0.7325   0.6412   0.4710

Si   T2     0.1602   0.5009   0.2558

Si   T2     0.1496   0.4852   0.8388

Si   T2     0.3240   0.4925   0.2614

Si   T2     0.1647   0.6667   0.2492

Si   T2     0.3191   0.8353   0.2183

Si   T2     0.3287   0.8359   0.7955

Si   T2     0.4916   0.8291   0.2296

Si   T2     0.4970   0.6701   0.8073

Si   T2     0.4972   0.8382   0.8090

Al   T2     0.3246   0.4868   0.8353

Al   T2     0.1545   0.6675   0.8180

Al   T2     0.4834   0.6568   0.2425

Si   T2     0.4961   0.1701   0.2449

Si   T2     0.4877   0.3312   0.7824

Si   T2     0.6588   0.1681   0.1843

Si   T2     0.8180   0.3365   0.7415

Si   T2     0.6537   0.4943   0.7547

Si   T2     0.8290   0.5047   0.7476

Si   T2     0.6648   0.5106   0.1777

Si   T2     0.4689   0.1610   0.8363

Si   T2     0.8358   0.3302   0.1619

Al   T2     0.4765   0.3365   0.1952

Al   T2     0.6447   0.1665   0.7589

Al   T2     0.8346   0.5127   0.1774

O    O1     0.2615   0.2663   0.5227

O    O1    -0.0001   0.7341   0.4943

O    O1     0.2610   0.9957   0.5071

O    O1     0.9788   0.2626   0.5028

O    O1     0.7230   0.7395   0.5162

O    O1     0.7121   1.0029   0.4870

O    O2     0.1539   0.3165   0.5803

O    O2     0.3233   0.1715   0.4227

O    O2     0.1608   0.8344   0.5469

O    O2     0.8180   0.1628   0.4540

O    O2     0.8409   0.6883   0.4814

O    O2     0.6705   0.8459   0.5308

O    O3     0.2606   0.5323   0.2686

O    O3     0.2477   0.5179   0.7982

O    O3     0.5117   0.2649   0.2529

O    O3     0.5209   0.2630   0.8096

O    O3     0.2621   0.7390   0.7549

O    O3     0.2675   0.7373   0.2711

O    O3     0.7389   0.2643   0.2093

O    O3     0.7173   0.2759   0.7246

O    O3     0.7264   0.4744   0.2296

O    O3     0.7291   0.4734   0.7146

O    O3     0.4453   0.7317   0.2731

O    O3     0.4682   0.7404   0.7628

O    O4     0.1031   0.4220   0.3738

O    O4     0.3137   0.4067   0.7008

O     O4     0.3994   0.3340   0.3289

O    O4     0.0794   0.4014   0.7507

O    O4     0.4375   0.1082   0.4016

O    O4     0.4070   0.2926   0.6580

O    O4     0.2811   0.4039   0.3597

O    O4     0.3790   0.1149   0.7481

O    O4     0.0831   0.6850   0.7044

O    O4     0.1114   0.6986   0.3580

O    O4     0.2962   0.8926   0.3346

O    O4     0.3137   0.9018   0.6827

O    O4     0.6770   0.0986   0.2755

O    O4     0.6681   0.1049   0.6237

O    O4     0.8695   0.3074   0.6156

O    O4     0.8966   0.3061   0.2683

O    O4     0.9008   0.6016   0.2974

O    O4     0.6685   0.5745   0.6420

O    O4     0.5814   0.7001   0.3527

O    O4     0.8878   0.5905   0.6438

O    O4     0.5689   0.8870   0.3565

O    O4     0.5859   0.7004   0.7069

O    O4     0.6900   0.6003   0.2601

O    O4     0.5834   0.9014   0.7063

O    O5     0.1546   0.5819   0.3423

O    O5     0.4215   0.5817   0.7125

O    O5     0.5717   0.4411   0.2768

O    O5     0.1371   0.5635   0.7339

O    O5     0.5865   0.1759   0.2932

O    O5     0.5677   0.4121   0.6808

O    O5     0.4093   0.5657   0.3676

O    O5     0.5314   0.1353   0.7079

O    O5     0.4217   0.8647   0.2935

O    O5     0.4231   0.8542   0.7368

O    O5     0.8410   0.4289   0.6586

O    O5     0.8528   0.4225   0.2602

O    O6     0.1330   0.4929   0.0476

O    O6     0.4723   0.3588   0.9727

O    O6     0.4696   0.1336   0.0409

O    O6     0.3503   0.4900   0.0592

O    O6     0.1419   0.6570   0.0451

O    O6     0.3318   0.8553   1.0103

O    O6     0.6358   0.1424   0.9828

O    O6     0.8499   0.3456   0.9506

O    O6     0.8520   0.5124   0.9526

O    O6     0.5008   0.6558   1.0123

O    O6     0.5097   0.8545   0.0229

O    O6     0.6471   0.5062   0.9669

K    K      0.6535   0.3388   0.4709

K    K      0.3165   0.6504   0.5416

D    D1     0.5058   0.1205   0.5843

D    D1     0.4205   0.5715   0.5750

D    D1     0.1170   0.5491   0.6101

D    D1     0.8655   0.4259   0.3894

D    D1     0.4371   0.8967   0.4057

D    D1     0.5631   0.4556   0.3979

D    D2     0.7769   0.7910   0.5334